Granular Material, Reclaimed Asphalt Pavement “RAP”

Spec	314 MUNI

S.P.

Option A – RAP to be used for shouldering

314.07		Construction

314.07.04 	Shoulders

ADD in the following:

100% Reclaimed Asphalt Pavement (RAP) material shall be used for final shoulders and rounding at the following locations in order of priority.

In the listed area(s), a 40 mm surface layer shall be placed.

The 100% Reclaimed Asphalt Pavement shall have 100% passing the 26.5 mm sieve.  RAP shall be stockpiled according to the requirements of OPSS 1150 MUNI.

314.09		Measurement for Payment

314.09.01	Actual Measurement

ADD in the following

314.09.01.02	Reclaimed Asphalt Pavement

Payment for the placement of reclaimed asphalt pavement shall be by the tonne.

314.10		Basis of Payment

ADD in the following:

314.10.03	Reclaimed Asphalt Pavement - Item

The Contractor shall be responsible for the method to weigh the material.  Tickets shall be supplied for payment. Payment at this unit rate shall include all costs associated with the screening, crushing, stockpiling, hauling, site preparation, placement, fine grading and compaction of the material.

Option B – RAP to be placed on roadway

314.07		Construction

314.07.01	Granular Subbase, Base and Surface

Add in the following:

All RAP material, upon being removed that is not utilized for shoulders and rounding, shall be delivered to the following locations:

The RAP to be placed to achieve a surface that is 0.1 m thick and 7.0 m wide.

The RAP shall be placed under conditions such that a smooth, well compacted, hard surface shall be achieved.  The 100% Reclaimed Asphalt Pavement shall have 100% passing the 26.5 mm sieve.  RAP shall be stockpiled according to the requirements of OPSS 1150.

Contractor to assume all remaining “RAP” not placed at identified locations shall be delivered to the Frobisher Depot. *designer to determine location. can be considered waste

Contractor is responsible to provide adequate equipment and labour to achieve the placement of the RAP and acceptable end product meeting City requirements.

* if placing both Shouldering and roadway utilize 314.09 and 314.10 from Option A

314.09		Measurement for Payment

314.09.01	Actual Measurement

ADD in the following

314.09.01.02	Reclaimed Asphalt Pavement

Payment for the placement of reclaimed asphalt pavement shall be by square meter.

314.10		Basis of Payment

ADD in the following:

314.10.03	Reclaimed Asphalt Pavement - Item

The Contractor shall be responsible for the method to weigh the material.  Tickets shall be supplied for payment. Payment at this unit rate shall include all costs associated with the screening, crushing, stockpiling, hauling, site preparation, placement, fine grading and compaction of the material.