Untreated Granular Subbase, Base, Surface, Shoulder and Stockpiling

Spec	314 MUNI

S.P.

314.02		References

Add in the following

OPSS 102	Weighing of Materials

314.05		Materials

314.05.02	Rap Shouldering

Delete in it’s entirety

Option A – RAP to be used for shouldering

314.07		Construction

314.07.04 	Shoulders

ADD in the following:

100% Reclaimed Asphalt Pavement (RAP) material shall be used for final shoulders and rounding at the following locations in order of priority.

- * insert location list here

In the listed area(s), a 40 mm surface layer shall be placed.

The 100% Reclaimed Asphalt Pavement shall have 100% passing the 26.5 mm sieve.  RAP shall be stockpiled according to the requirements of OPSS 1150 MUNI.

Placement of RAP shall not be carried out prior to June 1st and shall be completed no later than September 1st of the same year.

The work shall be carried out when the road is clean and free of standing water.  Placement shall not proceed in the rain or when the rain is in the immediate forecast.

314.09		Measurement for Payment

314.09.01	Actual Measurement

ADD in the following

314.09.01.02	Reclaimed Asphalt Pavement

Payment for the placement of reclaimed asphalt pavement shall be by the tonne.

314.10		Basis of Payment

ADD in the following:

314.10.03	Reclaimed Asphalt Pavement - Item

The Contractor shall be responsible for the method to weigh the material.  Tickets shall be supplied for payment. Payment at this unit rate shall include all costs associated with the screening, crushing, stockpiling, hauling, site preparation, placement, fine grading and compaction of the material.

Option B – RAP to be placed on roadway

314.07		Construction

314.07.01	Granular Subbase, Base and Surface

Add in the following:

All RAP material, upon being removed that is not utilized for shoulders and rounding, shall be delivered to the following locations:

    - * insert location list here

The RAP to be placed to achieve a surface that is 0.1 m thick and 7.0 m wide.

* Designer to confirm road width and thickness

The RAP shall be placed under conditions such that a smooth, well compacted, hard surface shall be achieved.  The 100% Reclaimed Asphalt Pavement shall have 100% passing the 26.5 mm sieve.  RAP shall be stockpiled according to the requirements of OPSS 1150.

Placement of RAP shall not be carried out prior to June 1st and shall be completed no later than September 1st of the same year.

The work shall be carried out when the road is clean and free of standing water.  Placement shall not proceed in the rain or when the rain is in the immediate forecast.

Contractor to assume all remaining “RAP” not placed at identified locations shall be delivered to. *designer to determine location.

Contractor is responsible to provide adequate equipment and labour to achieve the placement of the RAP and acceptable end product meeting City requirements.

* if placing both Shouldering and roadway utilize 314.09 and 314.10 from Option A

314.09		Measurement for Payment

314.09.01	Actual Measurement

ADD in the following

314.09.01.02	Reclaimed Asphalt Pavement

Payment for the placement of reclaimed asphalt pavement shall be by square meter at the specified thickness.

314.10		Basis of Payment

ADD in the following:

314.10.03	Reclaimed Asphalt Pavement - Item

The Contractor shall be responsible for the method to weigh the material.    Tickets shall be supplied for payment. Payment at this unit rate shall include all costs associated with the screening, crushing, stockpiling, hauling, site preparation, placement, fine grading and compaction of the material.